Application Note

Fabrication Specification

For Realtek WiFi 2 Layer moudle

Date: 2018/07/03

Version: 1.0

This document is subject to change without notice. The document contains Realtek confidential information and must not be disclosed to any third party without appropriate NDA.

AMEBAD 2-layers 0.8mm PCB fabricate note

- The PCB stack was show on Gerber file.

- The RF character impedance was 50ohm on RF trace width.

- PCB thickness  :  0.8mm

- stack : 2 Layer

| PCB Stack Up |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Layer | Type |  | Thickness (mil) |  |  | DK |
| Top side solder mask |  |  |  | 1.00 | mils |  |
| L1 | TOP | Differential & Signal | copper+plating | 1.40 | mils |  |
|  |  |  | core | 26.00 | mils | 4 |
| L2 | Bottom | Differential & Signal | copper+plating | 1.40 | mils |  |
| Bottom side solder mask |  |  |  | 1.00 | mils |  |
| TOTAL |  |  |  | 30.80 | mils |  |
|  |  |  |  | 0.58 | mm |  |

5.   RF  50 ohm Polar simulation :

  - RF Single trace

  - Unit : mils

  - USB differential pair : 90Ω

  - Unit :mils

6. Open/short test: all layers

7. Surface Finish : Electroless Ni/Au，ENIG

9. dielectric constant :4.3(FR4)